	Product
Super Fast Rectifier Diodes
	Type

GPCS27903-GU

8GEESG180-0200

	Metallization

Top Gold(30u”)   (
Bottom Gold(30u”)   (

	
[image: image1.wmf]B

A

1

2

D

F

E




	Dimension in millimeters

Dimension

A

1.80-0+0.03

B

1.33±0.03

C

0.10±0.03

D

0.310±0.02

E

0.030±0.01

F

0.040±0.02


	

	Absolute Maximum Ratings (Ta=25℃)

 PEAK REVERSE VOLTAGE  VRM .. 150 V         JUNCTION TEMPERATURE       Tj ..150℃ 

 PEAK FORWARD SURGE CURRENT  IFSM ….100 A      STORAGE TEMPERATURE RANGE  Tstg .. -65~150℃
Electrical Characteristics (sampling 100pcs per 1 lot)

Item

Symbol 

Test Condition

Standard

FORWARD VOLTAGE

VF

IF=3A

0.95 V (MAX)

REVERSE CURRENT

IR

VR=150V

1μA (MAX)

BREAKDOWN VOLTAGE

BVR

IR=5μA

200V(MIN) 

REVERSE RECOVERY TIME

TRR

RG1

30nsec 

Quality Assurance (sampling 100pcs per 1 lot)

Yield Assurance : 98%



	Ho Chien Electronics Inc.  
	Spec No.8GEESG180-0200
	DATE: May .23.2007 


C











_1061301590.vsd
B�

A�

1�

2�

�

D�

�

F�

E�


